TEAM BRIEFING · YOU ARE RUNNING OFAT

One-Factor-At-A-Time

The most common experimental strategy · you have freedom over what you run

You've been assigned the OFAT archetype. This is how most bench scientists actually run experiments: pick a baseline, vary one factor at a time, look at what happens, freeze the best value, move on to the next factor. It's intuitive. It's easy to explain.

You have full freedom over the values you test Unlike the other archetypes, your template contains NO pre-computed run list. You choose your baseline formulation and every subsequent experimental point yourself, guided by your chemistry intuition. You are running experiments the way most people naturally do — without a designed experiment.

The one rule — one factor at a time Every experiment must either replicate your current baseline or vary exactly ONE factor away from it. Never change two factors in the same run. This discipline is what makes your data 'OFAT' rather than 'random'.

What OFAT lets you see Every main effect, one at a time. If a factor has a monotonic effect on tensile, you'll find the direction. Under the assumption that factors are independent, you can combine per-factor bests into a joint prediction.

The system — what you're formulating

You are formulating a latex rubber film for a customer. There are five factors you can change and three responses you measure. Your facilitator will “run the experiment” and tell you the response values for any factor combination you submit.

| Factor | Coded range | Real-world range | Notes |
| --- | --- | --- | --- |
| latex_pct | -1 to +1 | 5 - 20 wt% | hard constraint: latex ≤ 20 wt% |
| crosslinker | -1 to +1 | 0.5 - 3.0 phr | phr = parts per hundred rubber |
| filler_loading | -1 to +1 | 0 - 40 phr | phr = parts per hundred rubber |
| cure_temp | -1 to +1 | 140 - 180 °C |  |
| cure_time | -1 to +1 | 5 - 30 min |  |

Responses returned by the each experiment:

tensile_mpa — tensile strength (MPa) — your target

elongation_pct — elongation at break (%)

hardness_shore_a — Shore A hardness

The rules and objective

Budget: 15 experiment-dollars — one submission = one dollar; the facilitator tracks this

Objective — maximize tensile_mpa

Infeasible submissions — if the facilitator tells you your combo is infeasible (e.g. crosslinker out of range), the facilitator will delete the row — no penalty if you made a typo; costs a dollar if you hadn't checked the constraint

No comparing notes with the other archetype teams — this is a competition; each team's answer is theirs to defend

Your runs sheet (in team-template-OFAT.xlsx)

The runs sheet is BLANK. It has rows waiting for you to fill in. The columns are:

run — row number (already filled in for you)

swept_factor — which factor you're varying in this run (or baseline or replicate) – to help you keep track of the “only vary one at a time” rule

5 factor columns — your five factor values in natural units, e.g. latex_pct=15, filler_phr=20, etc.

3 response columns — tensile / elongation / hardness — filled in by you as the facilitator reads them back

notes — anything you want to remember about this run

Suggested workflow

Step 1 — pick a baseline — Choose one formulation using your chemistry intuition. A common starting choice is the midpoint of every factor's range, but a chemistry-informed guess is fine too. Record it in row 1 with swept_factor = 'baseline'.

Step 2 — sweep one factor — Pick one factor. Choose levels across its range that you think will be informative. Run those experiments with all OTHER factors held at your baseline values. Fill in swept_factor with the factor's name.

Step 3 — read the response and note the best level — After you get responses, identify the level of that factor that gave the best tensile.

Step 4 — freeze at the best (or return to baseline) and move on — Purist OFAT: freeze at the best and move to the next factor. Some teams prefer to return to baseline between sweeps — either works, as long as each run set only varies ONE factor.

Step 5 — after all 15 experiments — Take the best-per-factor levels you observed, combine them into a joint prediction, and submit that as your predicted optimum in the analysis notebook.

How to submit a run

☐  Fill in one row of the run-log table 
☐  Ask facilitator for one or more results
     they will read back tensile, elongation, and hardness

☐  Record the responses in the same row
     the responses are what you'll fit your model to

☐  Repeat until you run out of budget
     or until you have all the data your design needs